%Data From:

%M.A.S.D. Barros, E.A. Silva, P.A. Arroyo, C.R.G. Tavares, R.M. Schneider, M. Suszek, E.F. Sousa-Aguiar, Removal of Cr(III) in the fixed bed column and batch reactors using as adsorbent zeolite NaX, Chem Eng Sci. 59 (2004) 5959–5966. https://doi.org/10.1016/j.ces.2004.07.040.

%Cr(III) on zeolite, fixed inlet concentration, 3 fluxes

Q=[7,9,11]/(60*1000000); %Flow rate [m^3/s]

%Isotherm values for c_eq, q_eq

ce=[0.3,0.95,1.45,1.89,2.89]*(52/3)e-3; %Adsorbate initial concentration [kg/m^3]

qe=[1.54,2.34,2.75,3.15,3.27]*(52/3)e-3; %Adsorbed fraction at equilibrium [kg/kg]

%Langmuir isotherm parameters

qm=0.0036*(52/3)e-3; %[kg adsorbate/kg adsorbent]

kL=2443.1; %[m^3solution/kgadsorbent]

qeexp=3.27*(52/3)e-3; %qe experimental

%Inlet concentration and t1/2 values for 3 fluxes

ci=0.018*(52/3)e-3; %Adsorbate initial concentration [kg/m^3]

t12=[1555.042017 1206.422018 976.9767442]*60; %Time at which the c/c_in=1/2 [s]

%3 sets of times for breakthrough data with 3 fluxes

texp={[1240	1300	1370	1435	1510	1670	1725	1765	1825	1880	1945	2005]*60,

[440	500	570	620	680	780	830	900	960	1030	1090	1140	1220	1290	1335	1465	1555	1945]*60,

[410	475	525	600	650	745	795	840	890	955	1025	1070	1160	1310]*60};

cexpci={[0	0	0	0.086642599	0.379061372	0.80866426	0.895306859	1	1	1	1	1],

[0.003610108 0.003610108 0.003610108 0.003610108 0.003610108 0.003610108 0.003610108 0.003610108 0.003610108 0.003610108 0.02166065  0.173285199 0.566787004 0.783393502 0.797833935 1.003610108 0.989169675 0.992779783],

[0.007220217 0.007220217 0.007220217 0.007220217 0.007220217 0.007220217 0.050541516 0.14801444  0.314079422 0.451263538 0.606498195 0.667870036 0.805054152 0.953068592]};

%Various operating parameters

Lb=8.8e-2; %Column height [m]

Db=0.9e-2; %Column diameter [m]

Sb=pi*(Db^2)/4; %Bed section area [m^2]

Vb=Sb*Lb; %Bed volume [m^3]

Pa=101325; %Atmospheric pressure [Pa]

T=30+273.15; %Column temperature 25 ºC [K]

rhoCr=7.19e3; %Adsorbate density at 26 ºC and 1.12 bar [kg/m^3]

MCr=52/1000; %Adsorbate Molecular Mass [kg/mol]

Rg=8.314; %Ideal gas constant [J/(K·mol)]

MH2O=0.018; %Water Molecular Mass [kg/mol]

muH2O=0.0008891; %Water dynamic viscosity [Pa·s]

rhoH2O=1000; %Water density [kg/m^3]

d=0.18e-3; %Particle diameter [m]

rhoac=880; %Adsorbent aparent density [kg/m^3] Calculated using rhoac=rhob/(1-e) with data from appfitCrLSQ

us=Q/Sb; %Initial superficial velocity [m/s]

mcoal=3e-3; %Mass of initial adsorbent [kg]

rhob=mcoal/Vb; %Bulk density [kg/m^3]

e=1-(rhob/rhoac); %Porosity of the bed [m^3void/m^3bed]

u=us/e; %Interstitial velocity [m/s]

kp=((d^2)/150)*(e^2)/((1-e)^2); %Permeability [m^2]